A 300 mm foundry silicon spin qubit unit cell exceeding 99 % fidelity in all operations

Nard Dumoulin Stuyck,1, 2  Paul Steinacker,1  Wee Han Lim,1, 2 Tuomo Tanttu,1, 2 MengKe Feng,1, 2 Andreas Nickl,1 Santiago Serrano,1, 2 Marco Candido,1 Jesus D. Cifuentes,1, 2 Fay E. Hudson,1, 2 Kok Wai Chan,1, 2 Stefan Kubicek,3 Julien Jussot,3 Yann Canvel,3 Sofie Beyne,3 Yosuke Shimura,3 Roger Loo,3 Clement Godfrin,3 Bart Raes,3 Sylvain Baudot,3 Danny Wan,3 Arne Laucht,1, 2 Chih Hwan Yang,1, 2 Andre Saraiva,2 Christopher C. Escott,2 Kristiaan De Greve,3, 4 and Andrew S. Dzurak1, 2

1School of Electrical Engineering and Telecommunications,

University of New South Wales, Sydney, NSW 2052, Australia

2Diraq, Sydney, NSW, Australia

3Imec, Leuven, Belgium

4Department of Electrical Engineering (ESAT), KU Leuven, Leuven, Belgium

Fabrication of quantum processors in advanced 300 mm wafer-scale complementary metal–oxide–semiconductor (CMOS) foundries provides a unique scaling pathway towards commercially viable quantum computing with potentially millions of qubits on a single chip. Here, we show precise qubit operation of a silicon two-qubit device made in a 300 mm semiconductor processing line. The key metrics including single- and two qubit control fidelities exceed 99 % and state preparation and measurement fidelity exceeds 99.9 %, as evidenced by gate set tomography (GST). We report coherence and lifetimes up to T2* = 30.4 µs, T2Hahn = 803 µs, and T1 = 6.3 s. Crucially, the dominant operational errors originate from residual nuclear spin carrying isotopes, solvable with further isotopic purification, rather than charge noise arising from the dielectric environment. Our results answer the longstanding question whether the favourable properties including high-fidelity operation and long coherence times can be preserved when transitioning from a tailored academic to an industrial semiconductor fabrication technology.

Figure 1, SQ6 logo. (Arial 10 Italic)

[1] C. H. Yang et al. Spin Qubit 6 (2024)

[2] De finibus bonorum et malorum (45 BCE) (Arial 11)